## Slide 1
Bionic Design and Additive Manufacturing of High-Performance Heat Sink
Yang Zhang, Junyuan Jiang, Yiwei Wang, Luying Xia
Supervisors: Dr. Yi Nie and Dr. Shanshan Long Aerospace Engineering, Department of Mechanical, Materials and Manufacturing
Structural Design
Heat sink: heat exchanger that dissipates the heat generated by an electronic or a mechanical device
Additive Manufacturing (AM): an industrial process that deposits materials layer by layer to create geometric 3D objects.
Motivation: To generate an innovative heat sink design that maximizes the benefits of additive manufacturing, particularly in terms of intricate geometries and robust materials.
Background and Motivation
Honeycomb arrangement of conical pins
Tree branches structure
Bionic design:
Contour of temperature distribution on the surface of the heat sink
Conical pins structure
Results & Analysis
A bionic heat sink: conical pins, honeycomb holes, raised branches, a honeycomb pattern, and enhanced aesthetic appeal.
The predicted figure of merit (FOM) was calculated to be 0.92264 W /(kg·K).
The aspect-ratio, 60-degree rule and minimal feature size were strictly followed to make the designed heat sink suitable for fabrication by binder jet additive manufacturing.
The Experimental FOM was measured to be 1.19 W /(kg·K), together with convincing error analysis.
1. The breakage of the pins impact on FOM 1.1% error
2. Chamfer of pins impact on FOM 9.2% error
3. Surface roughness of the printed model h coefficient
4. Heat transfer: Incomplete to heat sink.
Additive Manufacturing
Binder jetting metal additive manufacturing
Predicted FOM of the design heat sink
The performance of the designed heat sink is evaluated by the criterion called Figure of Merit (FOM):
(2)
where is the weight of the heat sink, and represent the measured heat resistance at 1and 5respectively. is the average temperature of the heat sink base, is the ambient temperature, and is the measured thermal power input.
AM of intricate geometries
Honeycomb and dendritic structure
Excellent heat dispassion ability by enhanced convection and contact area with air
Computational simulation
Experimental validation
Angle larger than 60 degrees to horizontal direction
Change to ellipse
chamfer
Aspect ratio smaller
than 6.7
Rebuild the model to ensure all the feature sizes are greater than 1.0 mm.
Modification of the design for binder jetting
Experiment set-up
Printed heat sink
Experimental and Simulated FOM of the design heat sink
Conclusions